## Slide 1: INTERNATIONAL MARINE CLAIMS CONFERENCE 2015
FAILED / ABORTED REPAIRS
WHO PAYS & WHY?
JOE GRASSO, ATTORNEY, WIGGIN & DANA
SEAN MURPHY, NAVAL ARCHITECT & SURVEYOR ATLANTIC MARINE ASSOCIATES

## Slide 2: What Constitutes “Failed”
EXAMPLE – STUCTURAL DAMAGE & REPAIRS
7 YEAR OLD TANKER

## Slide 3: The Original Damage

## Slide 4: The Original Damage
Damage found at Panama December 2013
Fractures:-
Around the rudder trunk;
Longitudinal frames fractured
Fractures between internal frames and shell plating
Rudder trunk plating fractured
Fractures between rudder horn and shell plating
A total of almost 8 metres of fractured structure

## Slide 5: The Original Damage

## Slide 6: The Original Permanent Repairs
Permanent repairs at the anchorage agreed by:-
Owners Representative(s)
Classification surveyors
Classification Welding Specialists
Hull & Machinery Surveyor
Competent Shore Contractor

## Slide 7: The Original Permanent Repairs
Cleaning the areas affected
Crack dye penetrant / ultrasound testing of the areas affected
Preparation (grinding / gouging) of the areas affected
Crack dye penetrant / ultrasound testing of the prepared areas
Preheating of the areas affected
Welding of the areas affected

## Slide 8: The Original Permanent Repairs
Inter welding-pass heating of the areas affected
Back gouging of the areas affected
Post heat treatment of the areas affected
Hardness measurements of the areas affected
Final weld testing.
3+ weeks to complete

## Slide 9: The Original Permanent Repairs

## Slide 10: The Original Permanent Repairs

## Slide 11: The Original Permanent Repairs

## Slide 12: The Original Permanent Repairs

## Slide 13: The Original Permanent Repairs
Ship re-enters service
Then four months later:-
Re-examination of repairs
Dye penetrant NDT
Further fracturing of the repaired areas
Classification issue further Condition of Class
Ship sails for drydock

## Slide 14: Repairs Fail

## Slide 15: Permanent Repairs - Again

## Slide 16: Permanent Repairs - Again

## Slide 17: Summary
Initial permanent repairs effected by a competent repairer following all procedures using approved techniques
Oversight by Classification with specialist welding knowledge
Nature and scope of repairs also agreed by Owners technical department and the Underwriters surveyor
No defects when the vessel sailed but the fractures re-appeared
Total costs four times the original estimate
Various other expensive cases; engines, machinery repairs etc.

## Slide 18: Questions?